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Technical Datasheet


SILICATE + SILICON EXTREME
Ready to use, silicate-silicone based, waterproof and self-cleaning organic render.
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Description
SILICATE + SILICONE EXTREME is 100% acrylic and highly flexible render. Features high colour stability following the drying process and limitless colour options in various final textured surfaces. Hassle-free application with trowel or rendering machine. Optimum adhesion to the substrate. A balanced formulation and high quality raw materials provide SILICATE + SILICONE EXTREME with outstanding qualities in application, individual design, extremely low water absorption and exceptional resistance to mechanical stresses.

Application examples
It is applied to all building materials such as: Exterior thermal insulation systems made of mineral wool, expanded and extruded polystyrene, concrete, plaster, cement boards, plasterboard, painted surfaces, silicone paints, silicate paints, acrylic paints, acrylic MDF. etc. Replaces the final coat of plaster and paint. Can be used for indoor and outdoor applications.

Advantages
· High elasticity resulting in minimizing cracking effects.
· For indoor and outdoor use.
· Excellent transpiration
· Highly resistant to algae and bacteria
· Highly resistant to water 
· Excellent behaviour under all weather conditions and ultraviolet radiation.
· Wide colour range
· Excellent colour stability.
· Excellent workability
· High bonding properties

Technical Specifications
Form: paste like acrylic silicate-silicone plaster
Density: 1.80 ± 0.03 Kg/L
Available granularity sizes: 1,0 mm, 1.5 mm
Colours: 1.000 hues from Bauer colour index and infinite other colour mixures
Water vapor permeability: V1
Water absorption:  W3
Adhesion: 0,4 MPa

Thermal conductivity:  λ=0.7 W/m K
Reactionto fire: Class A2-s1,d0

Substrate surface preparation
Make sure that surfaces are level and sufficiently firm.  Remove loose or detached fragments, dirt, oil, dust etc. Prior to material application, provide suitable preparation of the substrate and apply adhesion improving agent BAUER PRO 101. This way, uniform drying is ensured, resulting in uniform coating colour to all over the plastered surface. 

Mixture preparation
The material is ready for use after thorough stirring of its whole mass. 

Instructions for use
1) Application by hand
Apply plaster using stainless steel or plastic spatula, depending on plaster’s texture and finish requirements, other suitable tools may be used as well, e.g. brush, trowel, round brush, scraper etc. During application, avoid development of cavities. Thoroughly clean application tools before use to avoid development of spots on the surface. 

2) Application by spraying machine
SILICATE-SILICON Extreme can be also sprayed by mortar blaster. The application technique and the tools used may allow the development of considerable variety of the top surface.

Application is not recommended under extreme sunlight (temperature above 35oC) or rainfall and days when temperature is expected to drop below 5oC. After use remove material residues from tools using water while material is still fresh, or by other methods e.g. sanding or scraping when material has dried.

Curing time
Drying time depends on ambient temperature and relative humidity. Indicatively at 20 oC and with relative humidity 65% the product dries on the surface in about 6 hours.
Complete drying of the product is achieved in about 14 days. Drying time is extended to lower temperatures and / or higher relative humidity.

Maintenance
Plaster can be cleaned with water, using common household cleaning solutions. In case of using steam cleaners, the following conditions must be kept: 

Water pressure:   30-40 bar
Water temperature:  up to 30 oC
Distance from the spout:   30-50cm

Product specifications
Waterproof plaster SILICATE + SILICONE EXTREME is a certified organic plastering for exterior application, according to standard EN 15824.

Consumption
SILICATE + SILICON EXTREME 1,0 mm F 1.8 Kg/m2
SILICATE + SILICON EXTREME 1.5mm F 2.7 Kg/m2

Packaging
Plastic can, 25 Kg

Storage
Preferably in shady and sheltered area, protected against ice, high temperature and exposure to sunlight for at least 12 months. For more information regarding handling, storage and disposal of SILICATE + SILICON EXTREME plaster please refer to the EU material safety data sheet available to application professionals. The material's pot life is theoretically unlimited. Containers opened and reclosed may be reused after several months. 

Notes
Technical details, properties, recommendations and information on BAUER products are supplied in good faith. They are based on the company's research and experience, provided that they are stored and applied under normal conditions.  As the method of using materials as well as project and environment conditions are beyond the control of the company in each individual application setting, the product user is held solely responsible for the result of application. No responsibility under any legitimate relationship can be substantiated against the company, based on the information set out hereunder. Product users are advised to refer to the latest revision of the technical manuals available.












Other information

BAUER BUILDING TECHNOLOGIES
Megara Industrial Estate, Attica 
Tel: +30 210 5744222 
Fax: +30210 5740777 
Email:  info@netbauer.com
http// www.netbauer.com  
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